## Slide 1: From microstructural to macroscopic properties in failure of brittle heterogeneous materials
Laurent Ponson
Institut Jean le Rond d’Alembert
CNRS – Université Pierre et Marie Curie, Paris
Notes: Good morning
I would like to present you this recent work on the peeling properties of heterogeneous adhesives.
And show you through this example how we can bridge microscopic properties of brittle systems with their macroscopic effective failure properties.
I started this work as a post-doc at Caltech with my colleauges …. And I pursued it at Institut d’Alembert in Paris where I am currently working as a CNRS researcher.
Some background explanations: post-doc at Caltech where you did this work
Then, CNRS position when you pursued it.
You are interested by the failure properties of heterogeneous solids, and you develop new approaches in order to integrate the effect of material microstructure on their macroscopic failure properties

## Slide 2
s0
s0
Young’s modulus:
Eeff  average (Elocal)
Fracture energy:
Gceff  average (Gclocal)
X
Predicting the effective toughness of heterogeneous systems:
A challenging multi-scale problem
Notes: pour vous présenter la position du problème, considérons un matériau fissuré sous contrainte extérieure.

## Slide 3
s0
s0
Predicting the effective toughness of heterogeneous systems:
A challenging multi-scale problem
s (r)
r
Stress field diverges at the crack tip

## Slide 4
s0
s0
Predicting the effective toughness of heterogeneous systems:
A challenging multi-scale problem
s (r)
r
Macroscopic failure properties strongly dependent on material heterogeneities
Stress field diverges at the crack tip

## Slide 5
s0
s0
Macroscopic failure properties strongly dependent on material heterogeneities
Opens the door to microstructure design in order to achieve improved failure properties
Predicting the effective toughness of heterogeneous systems:
A challenging multi-scale problem
s (r)
r
Stress field diverges at the crack tip

## Slide 6
Application: Asymmetric adhesives
S. Xia, L. Ponson, G. Ravichandran and K. Bhattacharya, Phys. Rev. Lett. 2012 and International Patent 2011
Hard direction
Easy direction

## Slide 7
Goal: Developing a theoretical framework that predicts the
effective resistance of heterogeneous brittle systems
Using it for designing systems with improved failure properties
1- Theoretical approach: Equation of motion for a crack in an heterogeneous material
Failure as a depinning transition
2- Confrontation with experiments in the case of materials with disordered microstructures
Effective fracture energy of disordered materials
3- Application to material design in the context of thin film adhesives
Enhancement and asymmetry of peeling strength
Approach & outline:

## Slide 8
What are the effects of heterogeneities on the propagation of a crack?
z
x
Gext
1. Theory: deriving the equation of motion of a crack
Notes: coualitative

## Slide 9
What are the effects of heterogeneities on the propagation of a crack?
Pinning of the crack front:
z
x
Gext
1. Theory: deriving the equation of motion of a crack
Notes: coualitative

## Slide 10
Real material =
GC(M) = <GC> + δGc(M)
Homogeneous
material
Hypothesis:
-Brittle material
-Quasi-static crack
propagation
z
x
Gext
y
1. Theory: deriving the equation of motion of a crack
Fracture energy fluctuations
+

## Slide 11
Real material =
GC(M) = <GC> + δGc(M)
Fracture energy fluctuations
Homogeneous
material
+
Hypothesis:
-Brittle material
-Quasi-static crack
propagation
z
x
Gext
y
1. Theory: deriving the equation of motion of a crack
Random quenched noise with amplitude σGc
For disordered materials

## Slide 12
Elasticity of the material
Crack front as an elastic line:
Real material =
GC(M) = <GC> + δGc(M)
Homogeneous
material
z
x
f(z,t)
M
y
Gext
J. Rice (1985)
1. Theory: deriving the equation of motion of a crack
Fracture energy fluctuations
+

## Slide 13
Elasticity of the material
Crack front as an elastic line:
Real material =
GC(M) = <GC> + δGc(M)
Homogeneous
material
Equation of motion for a crack
z
x
M
y
Gext
L. B. Freund (1990)
J. Rice (1985)
1. Theory: deriving the equation of motion of a crack
f(z,t)
Fracture energy fluctuations
+

## Slide 14
Elasticity of the material
Crack front as an elastic line:
Real material =
GC(M) = <GC> + δGc(M)
Homogeneous
material
Equation of motion for a crack
z
x
M
y
Gext
J. Rice (1985)
1. Theory: deriving the equation of motion of a crack
J. Schmittbuhl et al. 1995, D. Bonamy et al. 2008, L. Ponson et al. 2010
f(z,t)
Fracture energy fluctuations
+

## Slide 15
Elasticity of the material
Crack front as an elastic line:
Real material =
GC(M) = <GC> + δGc(M)
Homogeneous
material
Equation of motion for a crack
z
x
M
y
Gext
J. Rice (1985)
1. Theory: deriving the equation of motion of a crack
Crack propagation as an elastic interface driven in a heterogeneous plane
f(z,t)
J. Schmittbuhl et al. 1995, D. Bonamy et al. 2008, L. Ponson et al. 2010
Fracture energy fluctuations
+

## Slide 16
Predictions on the dynamics of cracks
Gext
Gext
Variations of the average crack velocity with the external driving force
Vcrack
1. Theory: deriving the equation of motion of a crack
For disordered materials

## Slide 17
Predictions on the dynamics of cracks
Gext
Gext
Variations of the average crack velocity with the external driving force
Stable
Propagating
Toughening effect
Effective fracture energy:
Vcrack
1. Theory: deriving the equation of motion of a crack

## Slide 18
Predictions on the dynamics of cracks
Gext
Gext
Variations of the average crack velocity with the external driving force
Stable
Propagating
Toughening effect
Effective fracture energy:
Power law variation of the crack velocity
Crack velocity:
Vcrack
1. Theory: deriving the equation of motion of a crack

## Slide 19
Predictions on the dynamics of cracks
Gext
Gext
Variations of the average crack velocity with the external driving force
Stable
Propagating
Toughening effect
Effective fracture energy:
Power law variation of the crack velocity
Crack velocity:
Fluctuations of velocity
Intermittent dynamics of cracks
Power law distributed fluctuations of velocity
Vcrack
1. Theory: deriving the equation of motion of a crack

## Slide 20
Variations of the average crack velocity with the external driving force
2. Confrontation with experiments on disordered materials
Confrontation with experimental observations
Fracture test of a disordered brittle rock
L. Ponson, Phys. Rev. Lett. 2009

## Slide 21
Variations of the average crack velocity with the external driving force
2. Confrontation with experiments on disordered materials
Confrontation with experimental observations
Fracture test of a disordered brittle rock
L. Ponson, Phys. Rev. Lett. 2009
Critical regime

## Slide 22
Variations of the average crack velocity with the external driving force
L. Ponson, Phys. Rev. Lett. 2009
2. Confrontation with experiments on disordered materials
Confrontation with experimental observations
Fracture test of a disordered brittle rock
Subcritical regime
(thermally activated)
Critical regime

## Slide 23
Variations of crack velocity as a function of time
Fracture test of a disordered brittle rock
2. Confrontation with experiments on disordered materials
Confrontation with experimental observations
Définition of the size S of a fluctuation
Fluctuations of velocity
L. Ponson, Phys. Rev. Lett. 2009
Subcritical regime
(thermally activated)
Critical regime
Variations of the average crack velocity with the external driving force
D. Bonamy, S. Santucci and L. Ponson, Phys. Rev. Lett. 2008

## Slide 24
Variations of crack velocity as a function of time
Fracture test of a disordered brittle rock
2. Confrontation with experiments on disordered materials
Confrontation with experimental observations
Définition of the size S of a fluctuation
Fluctuations of velocity
L. Ponson, Phys. Rev. Lett. 2009
Subcritical regime
(thermally activated)
Critical regime
Variations of the average crack velocity with the external driving force
D. Bonamy, S. Santucci and L. Ponson, Phys. Rev. Lett. 2008

## Slide 25
Variations of crack velocity as a function of time
Fracture test of a disordered brittle rock
2. Confrontation with experiments on disordered materials
Confrontation with experimental observations
Définition of the size S of a fluctuation
Fluctuations of velocity
L. Ponson, Phys. Rev. Lett. 2009
Subcritical regime
(thermally activated)
Critical regime
Variations of the average crack velocity with the external driving force
Distribution of fluctuation sizes
Experimental results, Maloy, Santucci et al.
Theoretical predictions
P(S) ~ S-
with  ~ 1.65
D. Bonamy, S. Santucci and L. Ponson, Phys. Rev. Lett. 2008

## Slide 26
Variations of crack velocity as a function of time
Fracture test of a disordered brittle rock
2. Confrontation with experiments on disordered materials
Confrontation with experimental observations
Définition of the size S of a fluctuation
Fluctuations of velocity
L. Ponson, Phys. Rev. Lett. 2009
Subcritical regime
(thermally activated)
Critical regime
Variations of the average crack velocity with the external driving force
D. Bonamy, S. Santucci and L. Ponson, Phys. Rev. Lett. 2008
Distribution of fluctuation sizes
Experimental results, Maloy, Santucci et al.
Theoretical predictions
P(S) ~ S-
with  ~ 1.65
Failure of disordered brittle solids as a depinning transition

## Slide 27
Application: Effective fracture energy of disordered solids
Propagation direction
2. Effective fracture energy of disordered materials
Equation of motion of the crack
Fracture energy randomly distributed with standard deviation σGc

## Slide 28
Application: Effective fracture energy of disordered solids
Propagation direction
2. Effective fracture energy of disordered materials
Equation of motion of the crack
Effective fracture energy given by the depinning threshold
Fracture energy randomly distributed with standard deviation σGc
Effect of disorder strength σGc? Of its distribution (Gaussian, bivalued…)?
z

## Slide 29
2. Effective fracture energy of disordered materials
Theory: A simplified linear model inspired by Larkin
Propagation direction
A. Larkin and Y. Ovchinnikov (1979)

## Slide 30
2. Effective fracture energy of disordered materials
Theory: A simplified linear model inspired by Larkin
Validity range: so that
Propagation direction
A. Larkin and Y. Ovchinnikov (1979)
Front geometry
Larkin length
z
z

## Slide 31
2. Effective fracture energy of disordered materials
Theory: A simplified linear model inspired by Larkin
Validity range: so that
Typical resistance felt by a domain of size L
if L<ξ
if L<ξ
Propagation direction
A. Larkin and Y. Ovchinnikov (1979)
z
z
Front geometry
Larkin length

## Slide 32
2. Effective fracture energy of disordered materials
Theory: A simplified linear model inspired by Larkin
Validity range: so that
Typical resistance felt by a domain of size L
if L<ξ
if L<ξ
Larkin argument: critical depinning force set by the Larkin domains
Effective fracture energy
if
Individual pinning
Collective pinning
Propagation direction
if
A. Larkin and Y. Ovchinnikov (1979)
z
z
Front geometry
Larkin length

## Slide 33
2. Effective fracture energy of disordered materials
Simulations: collective vs individual pinning
V. Démery, A. Rosso and L. Ponson (2013)
Collective pinning
Individual pinning
Follows theoretical predictions
Depends on σGc only
Depends on more parameters (strongest impurities)

## Slide 34
2. Effective fracture energy of disordered materials
Simulations: collective vs individual pinning
V. Démery, A. Rosso and L. Ponson (2013)
Collective pinning
Individual pinning
Follows theoretical predictions
Depends on σGc only
Depends on more parameters (strongest impurities)
Disordered induced toughening relevant for the design of stronger solids

## Slide 35
Peeling of heterogeneous adhesives
M
f(z)
z
x
Equation of motion of the peeling front
3. Toughening and asymmetry in peeling of heterogeneous adhesives
Fp
Van Karman plate theory
Local driving force:
L. Ponson et al. (2013)

## Slide 36
Peeling of heterogeneous adhesives
M
f(z)
z
x
Equation of motion of the peeling front
Fp
Van Karman plate theory
Local driving force:
External driving force:
Displacement controlled
Hypothesis
Quasi-static propagation
Weakly heterogeneous
Brittle system
3. Toughening and asymmetry in peeling of heterogeneous adhesives
L. Ponson et al. (2013)

## Slide 37
Peeling of heterogeneous adhesives
M
f(z)
z
x
Equation of motion of the peeling front
Fp
Van Karman plate theory
Local driving force:
External driving force:
Displacement controlled
Local field of resistance:
if M belongs to a pinning site
elsewhere
3. Toughening and asymmetry in peeling of heterogeneous adhesives
L. Ponson et al. (2013)

## Slide 38
Peeling of heterogeneous adhesives
M
f(z)
z
x
Equation of motion of the peeling front
Fp
Van Karman plate theory
Local driving force:
External driving force:
Displacement controlled
Local field of resistance:
if M belongs to a pinning site
elsewhere
Similar to crack fronts in 3D elastic solids
Gext
J. Rice (1985)
3. Toughening and asymmetry in peeling of heterogeneous adhesives
L. Ponson et al. (2013)

## Slide 39
z
z
x
x
δf/d
Deformation of the front
Theoretical predictions
ContrastΔGc/Gc0
1.25
1.00
0.75
0.50
0.25
δf
Experiments on single defects: test of the approach
3. Toughening and asymmetry in peeling of heterogeneous adhesives

## Slide 40
z
z
x
x
δf
Experiments on single defects: test of the approach
3. Toughening and asymmetry in peeling of heterogeneous adhesives
Comparison with experiments
Δf/d
δf (μm)
z (mm)

## Slide 41
From the local field of fracture energy …
1. Theory: deriving an equation of motion for a peeling front

## Slide 42
… to the effective adhesion properties
1. Theory: deriving an equation of motion for a peeling front
M
f(z)
z
x
Peeling force G per unit length (N/m)
Average position of the peeling front (mm)
Peeling force G per unit length (N/m)
Average position of the peeling front (mm)
Effective peeling strength
Gmax

## Slide 43
… to the effective adhesion properties
1. Theory: deriving an equation of motion for a peeling front
M
f(z)
z
x
Peeling force G per unit length (N/m)
Average position of the peeling front (mm)
Peeling force G per unit length (N/m)
Average position of the peeling front (mm)
Gmax
Gmaxeasy
Gmaxhard
Average position of the peeling front (mm)
Peeling force G per unit length (N/m)
M
f(z)
z
x
Easy
direction
Hard direction
Strength asymmetry

## Slide 44
2. Confrontation with experiments on a model heterogeneous adhesive
Adhesive:
PDMS thin film produced by spin coating
Substrate:
Transparent sheet printed with a standard printer
Adhesion energy:
PDMS-ink
PDMS-transparent sheet
Gc1 = 12 J.m-2
Gc2 = 4 J.m-2
Contrast:
Gc1/Gc0 ≈ 3
Thickness between
100µm and 3mm
A model system for heterogeneous adhesion
Local field Gc(M) of local adhesion energy perfectly controled and known

## Slide 45
2. Confrontation with experiments on a model heterogeneous adhesive
Asymmetric adhesives
S. Xia, L. Ponson, G. Ravichandran and K. Bhattacharya, Phys. Rev. Lett. 2012 and international patent 2011
Hard direction
Easy direction

## Slide 46
Asymmetric adhesives
Hard direction
Easy direction
Optimization of the asymmetry by changing shape and contrast of pinning sites
2. Confrontation with experiments on a model heterogeneous adhesive
S. Xia, L. Ponson, G. Ravichandran and K. Bhattacharya, Phys. Rev. Lett. 2012 and international patent 2011

## Slide 47
3. Optimization and design of adhesives
Algorithm predicting Gmax from the local field Gc(x,z)
Genetic algorithm
A. Rosso and W. Krauth, PRE 2001
BIANCA algorithm, Vincenti et al., J. Glob. Opt. 2010
Elementary cell Lz x Lx
Defect
Front in the difficult direction
Front in the easy direction
Optimization procedure

## Slide 48
Optimization result
Thin defects with U shape
Gc1 as upper bound of Ghard
Gc0 as lower bound of Geasy
3. Optimization and design of adhesives
Asymmetry ≤ Gc1/Gc0

## Slide 49
Parametric study
3. Optimization and design of adhesives
Defect shape
z/d
f/d
Gc1
Gc0
Equilibrium shape of a front crossing a stripe with larger adhesion energy
M. Vasoya, J.B. Leblond and L. Ponson IJSS 2012
y/d

## Slide 50
Parametric study
3. Optimization and design of adhesives
Defect shape
f/d
Gc1
Gc0
Equilibrium shape of a front crossing a stripe with larger adhesion energy
M. Vasoya, J.B. Leblond and L. Ponson IJSS 2013
Contrast C = Gc1/Gc0
Defect width d/Ly normalized by the cell width
Asymmetry
y/d

## Slide 51
Beyond asymmetry:
how achieving enhanced peel strength

## Slide 52
Beyond asymmetry:
how achieving enhanced peel strength
Heterogeneities of adhesion energy
Effective peeling strength bonded by the max of the local Gc
Heterogeneities of elastic stiffness

## Slide 53
Adhesives with elastic heterogeneities: experimental study

## Slide 54
Adhesives with elastic heterogeneities: experimental study

## Slide 55
Dramatic increase of the effective peeling force
Adhesives with elastic heterogeneities: experimental study

## Slide 56
b
Peeling mechanism: homogeneous tape
Bending stiffness: D = EI
with moment of inertia: I = bh3/12

## Slide 57
Peeling mechanism: homogeneous tape
b
Bending stiffness: D = EI
with moment of inertia: I = bh3/12

## Slide 58
Peeling mechanism: homogeneous tape
b
Bending stiffness: D = EI
with moment of inertia: I = bh3/12

## Slide 59
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Peeling mechanism: homogeneous tape
b
Bending stiffness: D = EI
with moment of inertia: I = bh3/12

## Slide 60
F0 Δc (1-cosθ0)
Gc bΔc
X
Peeling mechanism: homogeneous tape
b
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Bending stiffness: D = EI
with moment of inertia: I = bh3/12

## Slide 61
F0 Δc (1-cosθ0)
Gc bΔc
X
Peeling mechanism: homogeneous tape
b
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Fc = bGc/(1-cosθ0)
Peeling force
R. S. Rivlin 1944
Bending stiffness: D = EI
with moment of inertia: I = bh3/12

## Slide 62
Simplest system that could give rise to toughening
One interface + inextensible tape
Toughening mechanism: heterogeneous tape

## Slide 63
Simplest system that could give rise to toughening
One interface + inextensible tape
Toughening mechanism: heterogeneous tape

## Slide 64
Simplest system that could give rise to toughening
One interface + inextensible tape
Toughening mechanism: heterogeneous tape

## Slide 65
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Simplest system that could give rise to toughening
One interface + inextensible tape
Toughening mechanism: heterogeneous tape

## Slide 66
Variation of the bending energy
Euler-Bernoulli beam theory
Simplest system that could give rise to toughening
One interface + inextensible tape
Toughening mechanism: heterogeneous tape
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:

## Slide 67
Simplest system that could give rise to toughening
One interface + inextensible tape
Toughening mechanism: heterogeneous tape
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Euler-Bernoulli beam theory

## Slide 68
Simplest system that could give rise to toughening
One interface + inextensible tape
Toughening mechanism: heterogeneous tape
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Euler-Bernoulli beam theory
h1/h2 = 2
Fhet /Fhom ≈ 8

## Slide 69
Adhesives with stripes of alternated stiffness
Adhesive described as a beam with alternating stiffness/bending rigidity
Work of the peel force used to bend the stiffer domains
Driven away from the peel front
S. Xia, L. Ponson, G. Ravichandran and K. Bhattacharya, J. Mech. Phys. Solids (2013)
For d>λb
d
Notes: So now, I would like to go beyond pinning of crack fronts by adhesion energy heterogeneities, and tell you a word about the effect of elastic properties heterogeneities

## Slide 70
Conclusions
Application: design of adhesives with new and improved properties
Effectives adhesion properties of thin films
Spatial distribution of heterogeneities at the microscale

## Slide 71
Acknowledgements
To my collaborators and student
To my sources of funding
Marie Curie fellowship (FP7 of European Union)
Integration grant (FP7 of European Union)
Shuman Xia, Guruswami Ravichandran, Kaushik Bhattacharya (Caltech)
Alberto Rosso (ENS, Paris)
Vincent Demery (Post-doc)

## Slide 72
…and perspectives
Toughening in 3D brittle solids
Extension of this theoretical framework to quasi-brittle solids
Induced by collective pinning for materials with a disordered microstructure
Effective resistance as a function of δGc
Induced by elastic heterogeneities, inspired by the adhesion enhancement mechanisms

## Slide 73
Direction of
propagation
K. Måløy et al. PRL 2006, D. Bonamy, S. Santucci and L. Ponson PRL 2008
Intermittent crack dynamics
Interaction between a crack front and material heterogeneties: dramatatic effects at all scales
Large scale roughness on fracture surfaces
Sandstone
L. Ponson et al. PRE 07
Silica glass
(courtesy of M. Ciccotti et al.)
.
Scale of heterogeneities in sandstone
Notes: Why is microstructure so important: because its effect is felt at all length scales
Here, two examples to illustrate this effect
(i) fracture surfaces:
Roughness with universal scaling properties observed at scales much larger than heterogeneity size in these materials
(ii) Crack dynamics:
Crack is observed to propagate through jumps with typical size much larger than heterogeneity size
Main question: how to bridge microscale properties of materials with their macroscopic failure properties

## Slide 74
The crack tip as a magnifying glass of the material heterogeneities
s0
s0
Notes: Difficulty:
Stress concentration at crack tip makes the system response very sensitive to the local properties of the material
As a result predicting macro scale properties of solids from their microscale characteristics is a very challenging task

## Slide 75
s (r)
r
The crack tip as a magnifying glass of the material heterogeneities
Stress fied diverges at the crack tip
s0
s0
Macroscopic response depends strongly on the material properties at the microstructure scale
Notes: Difficulty:
Stress concentration at crack tip makes the system response very sensitive to the local properties of the material
As a result predicting macro scale properties of solids from their microscale characteristics is a very challenging task

## Slide 76
s (r)
r
Stress fied diverges at the crack tip
s0
s0
Macroscopic response depends strongly on the material properties at the microstructure scale
The crack tip as a magnifying glass of the material heterogeneities
Opens the door to microstructure design in order to achieve improved failure properties
Notes: However, good news, this effect opens the door to the design of heterogeneous brittle solids with improved failure properties, by taking advantage of the interaction between the crack front and the material microstructure

## Slide 77
What are the effects of heterogeneities on the propagation of a crack?
z
x
Gext
1. Theory: deriving an equation of motion for a crack or a peeling front
Notes: coualitative

## Slide 78
What are the effects of heterogeneities on the propagation of a crack?
Pinning of the crack front:
z
x
Gext
1. Theory: deriving an equation of motion for a crack or a peeling front
Notes: coualitative

## Slide 79
Resistance of a real material
GC(M) = <GC> + δGc(M)
Fluctuating part
Average resistance
+
Hypothesis
Brittle material
Quasi-static propagation
Weakly heterogeneous
z
x
Gext
M
y
with <δGc>=0
1. Theory: deriving an equation of motion for a crack or a peeling front
=
.

## Slide 80
Elasticity of the material
Crack front as an elastic line:
z
x
f(z,t)
M
y
Gext
J. R. Rice (1985)
Resistance of a real material
Fluctuating part
Average resistance
+
=
GC(M) = <GC> + δGc(M)
with <δGc>=0
.
1. Theory: deriving an equation of motion for a crack or a peeling front

## Slide 81
Elasticity of the material
Crack front as an elastic line:
Equation of motion for a crack
z
x
M
y
Gext
L. B. Freund (1990)
J. R. Rice (1985)
GC(M) = <GC> + δGc(M)
Resistance of a real material
Fluctuating part
Average resistance
+
=
f(z,t)
with <δGc>=0
.
1. Theory: deriving an equation of motion for a crack or a peeling front

## Slide 82
Elasticity of the material
Crack front as an elastic line:
Equation of motion for a crack
z
x
M
y
Gext
J. R. Rice (1985)
J. Schmittbuhl et al. PRL 1995, L. Ponson PRL 2009, L. Ponson et al., IJF 2010
GC(M) = <GC> + δGc(M)
Resistance of a real material
Fluctuating part
Average resistance
+
=
f(z,t)
with <δGc>=0
.
1. Theory: deriving an equation of motion for a crack or a peeling front

## Slide 83
Peeling of an PDMS thin film from a printed heterogeneous substrate
2. Experiments: peeling of thin films with controlled heterogeneities
Experimental setup
Perturbation of the front: comparison theory/experiment
h=1.2mm
GcPDMS-ink = 1.4 J.m-2
GcPDMS-transparent = 6 J.m-2

## Slide 84
Experimental study of the effect of elastic heterogeneities
3. Application to the design of adhesives with improved properties
Notes: So now, I would like to go beyond pinning of crack fronts by adhesion energy heterogeneities, and tell you a word about the effect of elastic properties heterogeneities

## Slide 85
Experimental study of the effect of elastic heterogeneities
3. Application to the design of adhesives with improved properties
Notes: So now, I would like to go beyond pinning of crack fronts by adhesion energy heterogeneities, and tell you a word about the effect of elastic properties heterogeneities

## Slide 86
Experimental study of the effect of elastic heterogeneities
Dramatic increase of the effective peeling force
3. Application to the design of adhesives with improved properties
Notes: So now, I would like to go beyond pinning of crack fronts by adhesion energy heterogeneities, and tell you a word about the effect of elastic properties heterogeneities

## Slide 87
Bending stiffness: EI
Moment of inertia: I = bh3/12
Peeling mechanisms: homogeneous tape
b
3. Application to the design of adhesives with improved properties

## Slide 88
Bending stiffness: EI
Moment of inertia: I = bh3/12
Peeling mechanisms: homogeneous tape
3. Application to the design of adhesives with improved properties

## Slide 89
Bending stiffness: EI
Moment of inertia: I = bh3/12
Peeling mechanisms: homogeneous tape
3. Application to the design of adhesives with improved properties

## Slide 90
During the peeling process, for a propagation over Δc:
Bending stiffness: EI
Moment of inertia: I = bh3/12
R. S. Rivlin 1944
Peeling mechanisms: homogeneous tape
WF0 = ∆Es + ∆Eel
3. Application to the design of adhesives with improved properties

## Slide 91
WF0 = ∆Es + ∆Eel
F0 Δc (1-cosθ0)
Gc bΔc
X
Bending stiffness: EI
Moment of inertia: I = bh3/12
Peeling mechanisms: homogeneous tape
During the peeling process, for a propagation over Δc:
3. Application to the design of adhesives with improved properties

## Slide 92
WF0 = ∆Es + ∆Eel
F0 Δc (1-cosθ0)
Gc bΔc
X
Bending stiffness: EI
Moment of inertia: I = bh3/12
R. S. Rivlin 1944
Fc = bGc/(1-cosθ0)
Peeling force
Peeling mechanisms: homogeneous tape
During the peeling process, for a propagation over Δc:
3. Application to the design of adhesives with improved properties

## Slide 93
Simplest system susceptible to give rise to toughening
One interface + inextensible
Peeling mechanisms: heterogeneous tape
3. Application to the design of adhesives with improved properties

## Slide 94
Simplest system susceptible to give rise to toughening
One interface + inextensible
Peeling mechanisms: heterogeneous tape
3. Application to the design of adhesives with improved properties

## Slide 95
Simplest system susceptible to give rise to toughening
One interface + inextensible
Peeling mechanisms: heterogeneous tape
3. Application to the design of adhesives with improved properties

## Slide 96
Simplest system susceptible to give rise to toughening
One interface + inextensible
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Peeling mechanisms: heterogeneous tape
3. Application to the design of adhesives with improved properties

## Slide 97
Simplest system susceptible to give rise to toughening
One interface + inextensible
Variation of the bending energy
Euler-Bernoulli beam theory
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Peeling mechanisms: heterogeneous tape
3. Application to the design of adhesives with improved properties

## Slide 98
Simplest system susceptible to give rise to toughening
One interface + inextensible
Variation of the bending energy
Euler-Bernoulli beam theory
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
Peeling mechanisms: heterogeneous tape
3. Application to the design of adhesives with improved properties

## Slide 99
Simplest system susceptible to give rise to toughening
One interface + inextensible
Variation of the bending energy
Euler-Bernoulli beam theory
WF0 = ∆Es + ∆Eel
During the peeling process, for a propagation over Δc:
h1/h2 = 2
Fhet /Fhom = 8
Peeling mechanisms: heterogeneous tape
S. Xia, L. Ponson, G. Ravichandran and K. Bhattacharya (Submitted)
3. Application to the design of adhesives with improved properties

## Slide 100
Toughening mechanism: numerical investigation
S. Xia, L. Ponson, G. Ravichandran and K. Bhattacharya
US and international patent application 61/290, 133 (2010)
Finite element simulations with cohesive zone model
3. Application to the design of adhesives with improved properties

## Slide 101
Application: Effective fracture energy of disordered solids
Propagation direction
2. Effective fracture energy of disordered materials
Normalized equation of motion of the crack
Effective fracture energy given by the depinning threshold
Fracture energy fluctuations
distributed in P(gc)
Effect of disorder strength σ? Of its distribution P (Gaussian, bivalued…)?
z

## Slide 102
2. Effective fracture energy of disordered materials
A simplified (linear) model
Front geometry
Validity range: so that
Larkin length
Typical resistance felt by a domain of size L given by
if L<ξ
if L<ξ
Larkin argument: critical depinning force set by the Larkin domains
Effective fracture energy
if LLarkin<ξ
if LLarkin<ξ
Individual pinning
Collective pinning
Propagation direction