## Slide 1: The effect of electric field on crack formation patterns in drying laponite
Sujata Tarafdar
Jadavpur University
Kolkata, INDIA

## Slide 2: Collaborators:
Dibyendu Mal
Suparna Sinha
Tapati Dutta
Supti Sadhukhan
Soma Nag
Collaborators
Most of the recent work is done by
Tajkera Khatun (Sukhi)

## Slide 3
Thanks to DST-JSPS for
funding joint research
With Akio Nakahara,
So Kitsunezaki and their
Colleagues,
Indian collaborator:
Tapati Dutta
Spiral pattern
produced by
‘Memory Effect’
Matsuo and
Nakahara
J. Phys. Soc. Japan 81
(2012) 024801

## Slide 4
We are all familiar with Desiccation cracks in clay
Natural clay is not homogeneous
For experiments we choose
LAPONITE
a synthetic clay
Inhomogeneity in the system arises from
An Electric field acting on the system

## Slide 5
Some information about laponite.
Its particles are flat, disc-like and have a radius ~12 nm
And thickness ~ 1 nm.
Laponite structure and formula

## Slide 6
In water LAPONITE particles acquire
a negative charge
and it forms a GEL

## Slide 7
Laponite- methanol suspension – dried on-
Polypropylene
Glass

## Slide 8
Time development of cracks

## Slide 9
Rectangular sample of aqueous gel
(A) 47h:44m, (B) 71 h:47m and (C) 118h:53m

## Slide 10
To study the effect of an
electric field on the crack pattern
We adopt a setup with
Circular geometry
Rectangular geometry
Experiment:
7.5 gm of laponite +120 ml of distilled water,
stirred and poured into acrylic petri-dish/box

## Slide 11
Circular geometry
Metal foil
electrode

## Slide 12
20 cm
11.7 cm
RECTANGULAR GEOMETRY
Length-wise field
+ve
-ve
11.7 cm
+ve
-ve
Breadth-wise field
135 V
79 V
Produce same
field strength

## Slide 13
Results:
For CIRCULAR FIELD
Radial cracks appear
From center
Field is on for time 

## Slide 14
24 HRS
75 HRS
Center positive – 120 Volts, Al foil electrodes


## Slide 15
Center Negative
Radial cracks from boundary –
Cross Radial cracks near center

## Slide 16
Effect of varying  in Circular Geometry
a)Field on for 10 min
b) Field on for15 sec
c) Field on for 10 sec
d) Field on for 5 sec.
Center Positive
Field effect disappears

## Slide 17
Center Negative
=10 m, t=72h


=5 h
T= 70 h
It takes much
Longer time of
Field exposure ()
To induce
Pattern similar to
 

## Slide 18
Results for Rectangular field
Field is on for time 

## Slide 19
+ ve
After 84 h:12 m
Breadth-wise field
t = 18h:13min at +ve end
Field switched
Off after  2 min


## Slide 20
= 
Photo t = 51 h:19 m
 = 1h
Photo t = 69 h:36 m
E
+ve
Experiment in
plastic
Pencil box
Length-wise Field

## Slide 21
Observations:
Cracks run from +ve to –ve electrode
In rectangular system for  tree-like motifs form
For finite 
Cracks proceed
straighter

## Slide 22
Attempts to understand
these observations
We adapt spring network model
introduced earlier
(S Sadhukhan, S Roy Majumder, D Mal, T Dutta and S Tarafdar
J. Phys. Cond. Mat.19, 2008, 356206)
to include effect of the electric field
(T Khatun et al, PHYS REV E 86, 016114 , 2012)

## Slide 23: The 2-dimensional Spring network model
Each node on a square lattice represents a laponite particle
Springs with a certain spring constant (g) and Breaking threshold (s) connect nearest neighbors

## Slide 24
Red node moves under
force due to the 4
Springs connecting to
4 nearest neighbors
spring breaks
If strain threshold
S(i,j) is crossed
Spring connecting i and j
has stiffness g(i,j)
Force experienced by a laponite particle

## Slide 25: Desiccation Process
Desiccation is implemented by reducing the natural length of each spring in successive stages according to
d(n+1) = dn(1 – b/rn)
dn is natural length of spring at n’th
Stage, b and r are constants. This can be written as

## Slide 26
The net force gives the acceleration (a)
on the particle
It moves to new position at next time-step
x+1 = x + a t2
System relaxes for n steps before
next desiccation(here, n =1,
i.e quick drying compared
To relaxation assumed)

## Slide 27
Top view of a desiccating layer

## Slide 28
How to include force due to electric field ??
Embed square lattice
In a circular boundary
Case of circular geometry

## Slide 29
Simulated cracks in Circular Sample without electric field

## Slide 30
Total Force on each node :
Desiccation Force + Electric Force
Calculation of force due to imposed
Electric field
From radial symmetry of the setup,
we expect a net force towards/away from
The center

## Slide 31
ELECTRIC FIELD
Assume:
Laplace’s equation valid in the Laponite gel away from electrodes
Boundary Conditions potential φ is +V (−V ) at the inner electrode periphery and −V (+V) at the outer periphery.
φ has cylindrical symmetry
Potential map

## Slide 32
DIRECTION OF FORCE FIELD IN VECTOR MAP
-V
+V
+V
-V
Arrows show direction and magnitude of field

## Slide 33
V=20
V=10
Crack formation with nodes driven radially
away from center with force  electric field
V=20
V=10
V=5
V is proportional to field strength

## Slide 34
Small system (CP) with exaggerated distortion shows nodes pushed outward.
Cross-radially placed springs stretch and break, so radial cracks are formed.
Mechanism of formation of radial cracks

## Slide 35
NODES ARE DRIVEN TOWARDS THE CENTRE
V=20
V=10
V=5

## Slide 36
Small system (CN) with exaggerated distortion shows nodes pushed inward.
Radially placed springs stretch and break, so cross-radial cracks are formed.
Mechanism of formation of cross-radial cracks

## Slide 37
Notice a strong qualitative match in Patterns
Centre
-ve
Centre
+ve
Nodes forced
towards
center
Nodes forced
Away from
center
Are Laponite particles +ve charged ??

## Slide 38
There is a contradiction here
Clay macro-ions in colloidal solution are
Known to be –ve charged
A possible explanation -
Overcharging of macro-ions
in colloids

## Slide 39
Overcharging effect in colloids
Colloidal particles dissociate in water  macro-ions
with –ve surface charge +ve counterions.
Counterions form a double layer on the surface of the clay platelet, screening the bare charge.
Presence of multivalent cations can lead to a strong accumulation of opposite charge on the surface, which actually reverses the net charge on the macroion.
In our experiment Al3+ ions from anode may overcharge the laponite disks making them effectively +ve charged.
This counter-intuitive effect arises from strong
localization and interaction between Counter-ions

## Slide 40
Overcharged configuration has minimum energy –
More so for
larger macro-ions
Simulations demonstrating overcharging Ref: R. Messina, J. Phys.: Condens. Matter 21, 113102 (2009).

## Slide 41
Negative side
More indications of Overcharging
Thickening of the laponite film near the negative electrode.
In circular geometry
Ref: T. Khatun , M. D. Choudhury T. Dutta and S. Tarafdar , Phys. Rev. E 86, 016114 (2012)

## Slide 42
Initial solidification and shrinking at the +ve electrode
 , photo t = 20hr:38min
Thickening at –ve electrode, Photo t = 95hr:54min
+ve
-ve
Also observed in rectangular geometry

## Slide 43
We try a similar analysis for the
Rectangular system
Problem:
Boundary conditions at the sides
(normal to electrodes)
Are not well-defined
+V
-V
??
??

## Slide 44
20 cm
11.7 cm
+ve
-ve
A set-up with better
defined boundary conditions
+V
- V

## Slide 45
–ve electrode strongly corroded
Bubbles appear
Aluminum Electrodes
+ve
+ve

## Slide 46
Copper Electrodes
+ve electrode is strongly corroded
Cracks normal
To field
Cracks parallel
To field

## Slide 48
Crack growth in spring model assuming nodes are pushed along the field lines (i.e. the particles have effective positive charge).

## Slide 49
Alternating Field
AC fields of different strengths gave some
Peculiar effects in a circular set-up
Voltage was varied from 20 to 70 V at
Frequency 50 Hz

## Slide 50
20 Volts
After 17h:9min
After 23h:55min

## Slide 51
25 Volts
23h:50min
30 Volts
25h:4min
Pattern starts to change

## Slide 52
40 Volts
5h:52min
50 Volts
4h:29min

## Slide 53
50 Volts
Close-up
4h:42min
50 Volts
24h:24min

## Slide 54
70 volt field turned off after 4h:40min
Taken after 4h:40min
Then field switched off
After 22h:11min

## Slide 55
For higher fields there
was sparking and we were
scared to go on

## Slide 56
70 Volt AC in Rectangular sample

## Slide 57
AC applied along width

## Slide 58
Still a long way to go to understand
fully crack formation in electric fields ………
But lots of interesting results
to think about

## Slide 59
References
[1] D Mal, S Sinha, S Mitra and S Tarafdar Physica A, 346, 110, (2005)
[2] D Mal, S Sinha, T Dutta, S Mitra, S Tarafdar, Fractals, 14, 283 (2006)
[3] D Mal, S Sinha, T Dutta S Mitra, S Tarafdar, J. Phys. Soc. Jpn.76, 014801 (2006)
[4] D Mal, S Sinha, T Middya, S Tarafdar, Physica A 384 (2007)182
[5] D Mal, S Sinha, T Middya, S Tarafdar, Appl. Clay Science 39 (2008) 106
[6] S Sadhukhan, S Roy Majumder, D Mal, T Dutta and S Tarafdar
J. Phys. Cond. Mat.19, 2008, 356206
[7] S Sadhukhan, J Prehl, P Blaudeck, K H Hoffmann, T Dutta, S Tarafdar, Eur. Phys. J. E, 27 (2008) 391
[8] S Tarafdar, S Sinha, Ind. Eng. Chem. Res., Vol. 47, (2008) 6459
[9] Nag, S., Sinha, S., Sadhukhan, S., Dutta, T., Tarafdar, S. 2010
J. Phys. Cond Mat 22 (1), art. no. 015402
[10] Tajkera Khatun, Moutushi Dutta Choudhury, Tapati Dutta, Sujata Tarafdar, Phys. Rev. E 86 (2012), 016114

## Slide 60
Thank You